## Slide 1: Composite Panel – NASA ID CAR11C-9-2-Run1
8 plys
(0,90,0,90)s
Approximately 2 mm thick
Approximately 50 mm across
Height is greater than 50 mm- I would assume 100mm unless Cheryl has a different number
Based on CT Delamination Locations
  Between ply 1 and 2
  Between ply 2 and 3
  Between ply 3 and 4
  Between 5 and 6
  Between 6 and 7
Impact was on ply 8 by this numbering

## Slide 2: Delam1 - Between ply 1 and 2

## Slide 3: Delam2 - Between ply 2 and 3

## Slide 4: Delam3 - Between ply 3 and 4

## Slide 5: Delam4 - Between 5 and 6

## Slide 6: Delam5 - Between 6 and 7

## Slide 7: Data- compositeDelams.npz
cd=np.load('compositeDelams.npz')
cd.files=['delam3', 'delam1', 'delam5', 'delam4', 'delam2’
delam1.shape= (101, 247)
Zeros are delamination
Ones no delamination
Width (247) is full width of sample
Pixel size is 0.20 mm